66$)	Cubicle system $(kurz9Cubicle hardcell steel

$)

KEMMLIT UK
Bays Platt
Skirmett

Henley on Thames

Oxfordshire

RG9 6TD
Telephone: 01491 638606
info@kemmlituk.com - www.kemmlituk.com

Construction:

Asymmetric folded steel sheet sandwich element,

42 mm thick, hot-dip galvanised with a static connection

and vandal-resistant hardware.

TÜV-approved (GS seal of approval).

Options:
hardcell steel 1.1: Anodised aluminium profiles

hardcell steel 1.4: Stainless steel profiles

Height:
2000 mm, including 150 mm under panel clearance.
2135 mm, including 150 mm under panel clearance.

Other heights are also available.

Walls:
Steel sandwich element, 42 mm thick, hot-dip galvanised 
S 250 GD + Z-275 according to DVV, DIN EN 10142,
DIN EN 10147 and DIN EN 10143.

Visible polyester coating, approx. 25 µm thick white, grey,

metal grey  and black.  With additional protective varnish-coating

7-10 µm on the inside. 

Alternatively visible polyester coating in special crystal

effect approx. 50 (m thick. UV-resistant due to embedded

acrylic glass parts. In colours silverstar, redstar, bluestar,

brownstar and greenstar. With additional protective

varnish-coating on the inside 7-10 µm.

# The steel sheets are canted on all 4 sides.

The inside of the elements is filled with a warp-resistant

Inlay. Additional screw-proof inlays in the sandwich element

guarantee the long-lasting  and solid fixing of accessories.

# Profiles: 
The horizontal aluminium profile (frieze) does not run

# directly above the door front but rather is set back 220 mm.

# Alternatively stabilising profile (frieze) available in stainless steel.

Wall connections are accomplished by shadow gaps.

Supporting legs:
The supporting legs are set back 220 mm.

Made entirely of stainless steel with a diameter of 20mm.

Force-fit connection to the partition with M12 screw fitting.

The durable stainless

steel cover sleeve can easily be lifted for cleaning purposes.

Also available in corrosion-resistant aluminium,

satin anodised with stainless steel core and plate.

Durable cover sleeve made of anodised aluminium.

Cover sleeve can easily be lifted for cleaning purposes.

Doors:
Steel sandwich element 42 mm thick, hot-dip galvanised,

rebated (same construction as walls.

# Hinges:

2 robust, 2–roller-rising-butt-edge hinges made

of aluminium, (20 mm in diameter), for automatic

closing of the door, satin anodised.

Alternatively 2 robust 2-roller edge hinges- (20mm

in diameter), made of aluminium satin anodised.

# Alternatively decorative 2-roller edge hinges made of

# stainless steel (12 mm in diameter).

# Furniture/hardware:

Single latch lock WC, door knobs, red/white

indicator bolt with emergency release mechanism

made of satin anodised aluminium, in stainless

steel or impact- and shatter-resistant and colour-coordinated nylon.

Double latch lock WC, safety lever handle, 23 mm in diameter.

Red/white indicator bolt with emergency release mechanism

made of natural anodised aluminium, stainless steel

or impact and shatter-resistant and colour-coordinated

nylon.

Colours:
Colours of doors and walls according to the cell colour chart.

Environmental friendliness:
Only environmentally friendly materials without PVC

and CFCs must be used.

All prices ex works in Dusslingen. Taxes and duties

are unpaid, materials only. Installation and transportation

are not included.

$)

$(h1ii

$(lang Accessories for WC cubicles:

KEMMLIT-door stopper hooks made of  aluminium 401$)/E

$$NNN

$(h1ii66.20$)			$(menge0,000$) no.$(einhNo.$) $)	$(d276$)$(ep.............$)	$(gb.............

$)

$(langKEMMLIT-wall hooks made of aluminium 402$)/E

$$NNN

$(h1ii66.30$)			                             $(menge0,000$) no.$(einhNo.$) $)	$(d276$)$(ep.............$)	$(gb.............

$)

$(langKEMMLIT-paper roll holders made of aluminium 408$)/E

$$NNN

$(h1ii66.40$)			                             $(menge0,000$) no.$(einhNo.$) $)	$(d276$)$(ep.............$)	$(gb.............

$)

$(langKEMMLIT-replacement toilet roll holders made of aluminium 409$)/E

$$NNN

$(h1ii66.50$)			                             $(menge0,000$) no.$(einhNo.$) $)	$(d276$)$(ep.............$)	$(gb.............$)

$(langKEMMLIT-WC brush set made of aluminium 410
 $)/E$$NNN

$(h1ii66.60$)			                             $(menge0,000$) no.$(einhNo.$) $)	$(d276$)$(ep.............$)	$(gb.............

Accessories also available in stainless steel and nylon.

/E$$GRUEnd

----------------------

$(kurz9 Cubicle System hardcell steel $)	$(gb.............

$)	$(gb.............

$)

============/E